## Slide 1: Toward Optimized Membrane Unit Processes Via Multi-Scale Modeling David A. Ladner,1 Zuo Zhou,1 Colby Cash1
Salman Bin Kashif,2 Anna Malakian,2 Bowen Ling,3
Ilenia Battiato,3 Scott Husson,2 Sapna Sarupria2
1Environmental Engineering and Earth Sciences, Clemson University
2Chemical and Biomolecular Engineering, Clemson University
3Energy Resources Engineering, Stanford University
Notes: Speaker Name – Topic Title

## Slide 2: Patterned membranes are showing promise as foulant mitigators.

## Slide 3: This DMREF* project combined computational modeling with experiments to discover the best pattern geometries.
* DMREF: Designing Materials to Revolutionize and Engineer our Future

## Slide 4: Initial Ideas

## Slide 5: Biology is one source of inspiration.
Golovan et al., Phyl. Trans. Royal Soc. A, 2016. DOI: 10.1098/rsta.2016.0189.

## Slide 6: Lotus leaves are ultrahydrophobic and self-cleaning.
Depth: 0.256 mm, No fillets, CP factor=19
Depth: 0.256 mm, partial fillets, CP factor=13.7

## Slide 7: Shark-skin-inspired patterns result in low drag.
Depth: 0.256 mm CP factor=11.77
Depth: 0.128 mm CP factor=7.64

## Slide 8: Fabricate

## Slide 9: Polyamide thin-film composite membranes are patterned with a direct-press method.
Line & groove silicon stamp
Thermal embossing
Nanoscale patterning
PEGDE (5 wt% and 15 wt%)
Reaction
Chemical coating

## Slide 10: Woven mesh can also be used to generate patterns.
10x
40x

## Slide 11: Characterize and test

## Slide 12: SEM* allows us to visualize the quality of pattern imprinting.
*SEM: Scanning electron microscopy

## Slide 13: SEM allows us to visualize the quality of pattern imprinting.

## Slide 14: A LEXT* 3D Laser Measuring Microscope allows quantification of pattern depth and size.
5x
50x
20x
*LEXT: Product name with no acronym meaning (that we’ve found!).

## Slide 15: Confocal microscopy of stained membranes will allow us to visualize fouling patterns.
Stained patterned PVDF membrane
Stained pristine PVDF membrane

## Slide 16: Train Models
at multiple scales

## Slide 17: Our smallest-scale is at the molecular level. We model the membrane.
Each color represents
a different cluster.
Begin with a
polyamide cluster

## Slide 18: We also model the foulants at the molecular level.

## Slide 19: We scale up the modeling effort via CFD*.
Pattern length: 2 µm
Pattern length: 8 µm
Pattern length: 32 µm
Pattern length: 128 µm
Pattern length: 512 µm
*CFD: Computational fluid dynamics.

## Slide 20: CFD reveals how salt builds up within depressions.

## Slide 21: CFD reveals how patterns affect fluid flow and concentration polarization.
mol/m3

## Slide 22: We validate the CFD models using analytical results.

## Slide 23: CP increases as feature size increases.

## Slide 24: Flux improvements may be related to the increase in area.

## Slide 25: Boundary layer thickness correlates with roughness.

## Slide 26: We train the models by comparing fouling experiments to model results.

## Slide 27: Simulate Novel DeSigns

## Slide 28: We noticed some interesting behavior with the tire-tread pattern.

## Slide 29: The fouling pattern was flow-direction dependent (anisotropic).

## Slide 30: The pattern is able to make the flow field converge.

## Slide 31: Current and future efforts will move us up the helix.

## Slide 32: CFD is a useful tool for characterizing various unit processes.

## Slide 33: CFD is a useful tool for characterizing various unit processes.

## Slide 34: CFD is a useful tool for characterizing various unit processes.

## Slide 35: CFD is a useful tool for characterizing various unit processes.

## Slide 36: Acknowledgements
NSF
CBET-1236070
CBET-1534304
Research Group Website: http://davidladner.org
Clemson Light Imaging Facility
Clemson Electron Microscopy Facility
Palmetto Cluster